## Slide 2
Company history

## Slide 3
Company divisions
Thermoplastic Powders
Polyethylene Bags
Renewable energy

## Slide 4
European circular plastics production
Source: THE CIRCULAR ECONOMY FOR PLASTICS - A EUROPEAN ANALYSIS | 2024
In 2022, European production of circular plastics
reached 11.7 Mt. This accounted for 19.7% of European
plastics production in 2022.

## Slide 5
European plastics production evolution
Source: THE CIRCULAR ECONOMY FOR PLASTICS - A EUROPEAN ANALYSIS | 2024

## Slide 6
European plastics waste treatment
Source: THE CIRCULAR ECONOMY FOR PLASTICS - A EUROPEAN ANALYSIS | 2024

## Slide 7
LLDPE
from rotational molding
PE
from other molding process
Post-consumer recycled source in
Poliplast eco powders

## Slide 8
Rotomoulding recycled PE
SOURCE
rotomoulding waste
rotomoulding scrap
grinding
extrusion and filtration
98% RECYCLED MATERIAL

## Slide 9
Rotomoulding recycled PE
material availability based on customer collection
limited colors, available mainly in black
high % recycled material
98% RECYCLED MATERIAL
composed only of rotomoulded PE

## Slide 10
New ECO PE
good supply chain
OUR FOCUS:
many colors
certified products
new applications for recycled products
various % of recycled material
different source of recycled material

## Slide 11
New ECO PE
waste recovery
LLDPE film
Also collected by:

## Slide 12
New ECO PE
selection
grinding
separation by color
material selection
reduction into small parts

## Slide 13
New ECO PE
washing
drying
reduced water consumption
water-purifying plant
minimum humidity for better extrusion process

## Slide 14
New ECO PE
Extrusion and filtration
granule mixing
melt filtration at 80 microns
homogeneous material
uniform color

## Slide 15
New ECO PE color range
ECO 30%
ECO 50%

## Slide 16
ECO PRODUCTS
CERTIFIED,PLASTICA SECONDA VITA
medium density and high mfi
better mouldability
medium density and medium mfi
for general use
high density grade
with greater flexural modulus
30% RECYCLED MATERIAL

## Slide 17
ECO PRODUCTS
CERTIFIED,PLASTICA SECONDA VITA
low mfi
medium density
high density grade
better mouldability
50% RECYCLED MATERIAL

## Slide 18
Certificate ,PLASTICA SECONDA VITA
PSV Mix Eco label: for materials and products
obtained from mixtures of materials obtained from:
separate waste collection and/or industrial residues
having a minimum content of recycled plastics of 30%

## Slide 19
Certificate ,PLASTICA SECONDA VITA

## Slide 20
APPROVED by EU COMMISSION

## Slide 21
EUROPEAN PLATFORM
PolyCert Europe is an umbrella technical platform harmonising existing certification schemes for converters of polymeric materials in Europe. The objective of PolyCert Europe is to provide quality certification and verification of recycled content in converted products.

## Slide 22
Weathering test – color deviation

## Slide 23
Rgb values
Coverage 2 and 4mm
Color deviation
Technical data sheet
2023
start test up to 5000h
Test for EACH COLOR

## Slide 24
Weathering test – mechanical properties

## Slide 25
Weathering test – mechanical properties

## Slide 26
Thanks for the attention